| Structure Id |  |  |  |  |  |  |  | Name |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 8086 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Crossing Name |  |  |  |  |  |  |  | Alt. Name |  |  |  |  |  |  |
| Smothering Creek |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Structure Type |  |  |  |  |  |  |  | Owner |  |  |  |  |  |  |
| Bridge |  |  |  |  |  |  |  | TMR Department of Transport & Main Roads |  |  |  |  |  |  |
| Construction Type |  |  |  |  |  |  |  | District |  |  |  |  |  |  |
| Girder/Beam |  |  |  |  |  |  |  | 12 - Wide Bay District |  |  |  |  |  |  |
| Construction Material |  |  |  |  |  |  |  | LGA Id |  |  |  |  |  |  |
| Timber |  |  |  |  |  |  |  | 228 - Fraser Coast Regional Council |  |  |  |  |  |  |
| Inspector |  |  |  |  |  |  |  | Date |  |  |  |  |  |  |
| Evan T Matthews |  |  |  |  |  |  |  | 18/05/2015 |  |  |  |  |  |  |
| Inspection |  | Level 2 |  |  | Programmed |  |  |  |  |  | All Elements Drilled |  |  |  |
|  |  | Level 3 |  |  | Exceptional |  |  |  |  |  | Underwater |  |  |  |
| Road Section |  |  |  |  |  |  |  | Start |  | End |  |  | TDist |  |
| Id | Description |  | S | Cway |  |  | S | RPC | Dist | RPC |  | Dist | Start | End |
| 487 | BROOWEENA - WO |  | C | 1 |  |  | C | 4 | 0.000 | 4 |  | 0.018 | 28.151 | 28.169 |

| * Test Locations |  |  | % Consumed |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | CS 2 |  | CS 3 |  | CS 4 |  |
| Component | Defect | Location (Abbreviation) (Describe Other (O) in comments) | E | MS | E | MS | E | MS |
| Pile | Pipe | Top (T), Ground Level (GL), (O) Other | 1-20 | 1-20 | 21-35 | 21-35 | 36-50 | 36-50 |
| Girder | Pipe | End1 (E1), Midspan (MS), End 2 (E2), Other (O) | 1-20 | 1-30 | 21-35 | 31-50 | 36-50 | 51-70 |
| Corbel | Pipe | End1 (E1), End 2 (E2), Other (O) | 1-20 | 1-20 | 21-35 | 21-35 | 36-50 | 36-50 |
| Headstock | Edge Area | End1 (E1), End 2 (E2), Other (O) | 1-5 | 1-5 | 6-10 | 6-10 | 11-20 | 11-20 |
| Headstock | Pipe | End1 (E1), End 2 (E2), Other (O) | 1 - 45mm |  | 46 - 65mm |  | 66 - 90mm |  |
| Other Component - Enter relevant component code and describe location in comments field. - Area of headstock (%) for external loss of section (top, bottom or sides). - Maximum pipe diameter (mm) in headstock for internal piping defects. - Members in excess of CS4 deterioration are critical and should be replaced immediately. |  |  |  |  |  |  |  |  |

| Structure Id |  |  |  | Name |  |  |  |  |  | Inspection date |  |  |  |  | Inspection Level |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 8086 |  |  |  |  |  |  |  |  |  | 18/05/2016 |  |  |  |  | 2 |  | 3 |  | Programmed |  |  |  | Exceptional |  |  | All Elements Drilled |  | Underwater |
| Location |  |  |  |  |  |  | Test Details |  |  |  |  | Test Results |  |  |  | % Consumed |  | Condition State |  | Undersize | Snipe Depth | Comments |  |  |  |  |  |  |
| Modification | Group | Component | Standard Number |  | Diameter (mm) |  | Location | Diameter | Orientation (H, V, Other) |  |  | Solid | Rot | Pipe |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| O | A1 | H1 | 54 |  | 300 |  | E1 | 10 | V |  |  | 300 |  |  |  | 0 |  | 1 |  |  |  | Treated, bands & end caps fitted both ends |  |  |  |  |  |  |
| O | A1 | H1 | 54 |  | 300 |  | O1 | 10 | V |  |  | 300 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound at P2 & P3 |  |  |  |  |  |  |
| O | A1 | H1 | 54 |  | 300 |  | E2 | 10 | V |  |  | 300 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A1 | H2 | 54 |  | 210 |  | E1 | 10 | H |  |  | 210 |  |  |  | 0 |  | 1 |  |  |  | Treated, bands & end caps fitted both ends |  |  |  |  |  |  |
| O | A1 | H2 | 54 |  | 210 |  | O1 | 10 | H |  |  | 210 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound at P2 & P3 |  |  |  |  |  |  |
| O | A1 | H2 | 54 |  | 210 |  | E2 | 10 | H |  |  | 210 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A1 | P1 | 60 |  | 320 |  | T | 10 | H |  |  | 150 |  | 170 |  | 53 |  | 4 |  |  |  | 600mm visible |  |  |  |  |  |  |
| O | A1 | P1 | 60 |  | 360 |  | T | 10 | O |  |  | 220 |  | 140 |  | 39 |  | 4 |  |  |  | Cracking to 11mm |  |  |  |  |  |  |
| O | A1 | P1 | 60 |  | 330 |  | GL | 10 | H |  |  | 330 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A1 | P1 | 56 |  | 320 |  | T | 10 | H |  |  | 320 |  |  |  | 0 |  | 1 |  |  |  | CS2 Cracking (only 200mm visible) |  |  |  |  |  |  |
| O | A1 | P1 | 56 |  | 320 |  | T | 10 | O |  |  | 320 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A1 | P2 | 56 |  | 355 |  | T | 10 | H |  |  | 355 |  |  |  | 0 |  | 1 |  |  |  | CS2 Cracking (only 200mm visible) |  |  |  |  |  |  |
| O | A1 | P2 | 56 |  | 355 |  | T | 10 | O |  |  | 355 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A1 | P3 | 56 |  | 430 |  | T | 10 | H |  |  | 430 |  |  |  | 0 |  | 1 |  |  |  | CS2 Cracking (only 200mm visible) |  |  |  |  |  |  |
| O | A1 | P3 | 56 |  | 420 |  | T | 10 | O |  |  | 420 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A1 | P4 | 56 |  | 360 |  | T | 10 | H |  |  | 360 |  |  |  | 0 |  | 1 |  |  |  | CS2 Cracking (only 200mm visible) |  |  |  |  |  |  |
| O | A1 | P4 | 56 |  | 350 |  | T | 10 | O |  |  | 350 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A1 | P2 | 60 |  | 300 |  | T | 10 | H |  |  | 300 |  |  |  | 0 |  | 1 |  |  |  | CS2 Minor fire damage (1m visible) |  |  |  |  |  |  |
| O | A1 | P2 | 60 |  | 310 |  | T | 10 | O |  |  | 310 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G1 | 22 |  | 360 |  | E1 | 10 | H |  |  | 360 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound on very end, 100mm from ABS |  |  |  |  |  |  |
| O | S1 | G1 | 22 |  | 405 |  | O | 10 | H |  |  | 355 |  | 50 |  | 12 |  | 2 |  |  |  | Drilled on very end, 100mm from ABS |  |  |  |  |  |  |
| O | S1 | G1 | 22 |  | 350 |  | S1 |  |  |  |  |  |  |  |  |  |  | 4 |  |  | 100 | CS2, Bands fitted. 25mm packer between girder & h/stock |  |  |  |  |  |  |
| O | S1 | G1 | 22 |  | 360 |  | MS | 10 | H |  |  | 360 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G1 | 22 |  | 335 |  | MS | 10 | V |  |  | 335 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G1 | 22 |  | 360 |  | E2 | 10 | H |  |  | 360 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G1 | 22 |  | 350 |  | S2 |  |  |  |  |  |  |  |  |  |  | 3 |  |  | 50 | CS2 Bands fitted |  |  |  |  |  |  |
| O | S1 | G3 | 22 |  | 400 |  | O | 10 | H |  |  | 280 |  | 120 |  | 30 |  | 2 |  |  |  | Drilled on very end, 100mm from ABS |  |  |  |  |  |  |
| O | S1 | G2 | 22 |  | 405 |  | E1 | 10 | H |  |  | 355 |  | 50 |  | 12 |  | 2 |  |  |  | Pipes could possibly be cracks |  |  |  |  |  |  |
| O | S1 | G2 | 22 |  | 385 |  | E1 | 10 | V |  |  | 355 |  | 50 |  | 13 |  | 2 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G2 | 22 |  | 385 |  | S1 |  |  |  |  |  |  |  |  |  |  | 2 |  |  | 30 |  |  |  |  |  |  |  |
| O | S1 | G2 | 22 |  | 405 |  | MS | 10 | H |  |  | 405 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G2 | 22 |  | 405 |  | MS | 10 | V |  |  | 405 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G2 | 22 |  | 405 |  | S2 |  |  |  |  |  |  |  |  |  |  | 2 |  |  | 30 |  |  |  |  |  |  |  |
| O | S1 | G3 | 22 |  | 375 |  | O | 10 | O |  |  | 285 |  | 90 |  | 24 |  | 2 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G3 | 22 |  | 400 |  | E1 | 10 | H |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G3 | 22 |  | 375 |  | S1 |  |  |  |  |  |  |  |  |  |  | 1 |  |  | 20 |  |  |  |  |  |  |  |
| O | S1 | G3 | 22 |  | 390 |  | MS | 10 | H |  |  | 390 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G3 | 22 |  | 390 |  | MS | 10 | V |  |  | 390 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G3 | 22 |  | 390 |  | E2 | 10 | H |  |  | 390 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G3 | 22 |  | 390 |  | S2 |  |  |  |  |  |  |  |  |  |  | 1 |  |  | 20 |  |  |  |  |  |  |  |
| O | S1 | G4 | 22 |  | 375 |  | E1 | 10 | H |  |  | 375 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound on very end, 100mm from ABS |  |  |  |  |  |  |
| O | S1 | G4 | 22 |  | 370 |  | S1 |  |  |  |  |  |  |  |  |  |  | 1 |  |  | 20 |  |  |  |  |  |  |  |
| O | S1 | G4 | 22 |  | 385 |  | MS | 10 | H |  |  | 385 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G4 | 22 |  | 390 |  | MS | 10 | V |  |  | 390 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G4 | 22 |  | 400 |  | E2 | 10 | H |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G4 | 22 |  | 405 |  | S2 |  |  |  |  |  |  |  |  |  |  | 2 |  |  | 35 |  |  |  |  |  |  |  |
| O | S1 | G5 | 22 |  | 400 |  | E1 | 10 | H |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  | CS2 Sawn & treated. Drilled sound on very end, 100mm from ABS |  |  |  |  |  |  |
| O | S1 | G5 | 22 |  | 385 |  | E1 | 10 | V |  |  | 385 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G5 | 22 |  | 385 |  | S1 |  |  |  |  |  |  |  |  |  |  | 1 |  |  | 20 |  |  |  |  |  |  |  |
| O | S1 | G5 | 22 |  | 405 |  | MS | 10 | H |  |  | 405 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G5 | 22 |  | 400 |  | MS | 10 | V |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G5 | 22 |  | 350 |  | E2 | 10 | H |  |  | 410 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S1 | G5 | 22 |  | 280 |  | E2 | 10 | V |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | COR1 | 27 |  | 350 |  | E1 | 10 | H |  |  | 350 |  |  |  | 0 |  | 1 |  |  |  | Gang nails fitted on both ends |  |  |  |  |  |  |
| O | P1 | COR1 | 27 |  | 280 |  | E1 | 10 | V |  |  | 280 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | COR1 | 27 |  | 350 |  | O | 10 | H |  |  | 350 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound mid-cor. |  |  |  |  |  |  |
| O | P1 | COR1 | 27 |  | 350 |  | E2 | 10 | H |  |  | 350 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | COR1 | 27 |  | 280 |  | E2 | 10 | V |  |  | 280 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | COR2 | 27 |  | 380 |  | E1 | 10 | H |  |  | 380 |  |  |  | 0 |  | 1 |  |  |  | Sawn, treated. Bands & gang nails fitted both ends |  |  |  |  |  |  |
| O | P1 | COR2 | 27 |  | 330 |  | E1 | 10 | V |  |  | 330 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | COR2 | 27 |  | 380 |  | O | 10 | H |  |  | 380 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound mid-cor. |  |  |  |  |  |  |
| O | P1 | COR2 | 27 |  | 380 |  | E2 | 10 | H |  |  | 380 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | COR2 | 27 |  | 345 |  | E2 | 10 | V |  |  | 345 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | COR3 | 27 |  | 385 |  | E1 | 10 | H |  |  | 385 |  |  |  | 0 |  | 1 |  |  |  | Sawn, treated. Bands & gang nails fitted both ends |  |  |  |  |  |  |
| O | P1 | COR3 | 27 |  | 335 |  | E1 | 10 | V |  |  | 335 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | COR3 | 27 |  | 385 |  | O | 10 | H |  |  | 385 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound mid-cor. |  |  |  |  |  |  |
| O | P1 | COR3 | 27 |  | 385 |  | E2 | 10 | H |  |  | 385 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | COR3 | 27 |  | 335 |  | E2 | 10 | V |  |  | 335 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | COR4 | 27 |  | 380 |  | E1 | 10 | H |  |  | 380 |  |  |  | 0 |  | 1 |  |  |  | CS1 Sawn & treated. Bands & gang nails fitted both ends |  |  |  |  |  |  |
| O | P1 | COR4 | 27 |  | 330 |  | E1 | 10 | V |  |  | 330 |  |  |  | 0 |  | 1 |  |  |  | 10mm packer between COR & H1 only. |  |  |  |  |  |  |
| O | P1 | COR4 | 27 |  | 380 |  | O | 10 | H |  |  | 380 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound mid-cor. |  |  |  |  |  |  |
| O | P1 | COR4 | 27 |  | 380 |  | E2 | 10 | H |  |  | 380 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | COR4 | 27 |  | 330 |  | E2 | 10 | V |  |  | 330 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | COR5 | 27 |  | 360 |  | E1 | 10 | H |  |  | 360 |  |  |  | 0 |  | 1 |  |  |  | Gang nails fitted on both ends |  |  |  |  |  |  |
| O | P1 | COR5 | 27 |  | 270 |  | E1 | 10 | V |  |  | 270 |  |  |  | 0 |  | 1 |  |  |  | CS2 15mm packer between COR & H1 only. |  |  |  |  |  |  |
| O | P1 | COR5 | 27 |  | 360 |  | O | 10 | H |  |  | 360 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound mid-cor. |  |  |  |  |  |  |
| O | P1 | COR5 | 27 |  | 340 |  | E2 | 10 | H |  |  | 340 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | COR5 | 54 |  | 290 |  | E2 | 10 | V |  |  | 290 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | H1 | 54 |  | 210 |  | E1 | 10 | H |  |  | 210 |  |  |  | 0 |  | 2 |  |  |  | CS2 Treated. Cracking into connection. Bands & end cap fitted |  |  |  |  |  |  |
| O | P1 | H1 | 54 |  | 210 |  | O1 | 10 | H |  |  | 210 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound at P2 & P3 |  |  |  |  |  |  |
| O | P1 | H1 | 54 |  | 210 |  | E2 | 10 | H |  |  | 210 |  |  |  | 0 |  | 2 |  |  |  | Cracking into connections. Bands & end caps fitted |  |  |  |  |  |  |
| O | P1 | H2 | 54 |  | 210 |  | E1 | 10 | H |  |  | 210 |  |  |  | 0 |  | 1 |  |  |  | Treated. Bands & end caps fitted both ends |  |  |  |  |  |  |
| O | P1 | H2 | 54 |  | 210 |  | O2 | 10 | H |  |  | 210 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound at P1 & P2 |  |  |  |  |  |  |
| O | P1 | H2 | 54 |  | 210 |  | E2 | 10 | H |  |  | 210 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | P1 | 56 |  | 355 |  | T | 10 | H |  |  | 355 |  |  |  | 0 |  | 1 |  |  |  | CS2 Butt spliced 800mm above GL (4 x plates fitted) |  |  |  |  |  |  |
| O | P1 | P1 | 56 |  | 340 |  | T | 10 | O |  |  | 340 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound above & below splice |  |  |  |  |  |  |
| O | P1 | P1 | 56 |  | 350 |  | GL | 10 | H |  |  | 350 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | P1 | 56 |  | 370 |  | GL | 10 | O |  |  | 370 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | P2 | 56 |  | 400 |  | T | 10 | H |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  | CS2 Sap loss throughout |  |  |  |  |  |  |
| O | P1 | P2 | 56 |  | 390 |  | T | 10 | O |  |  | 390 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | P2 | 56 |  | 380 |  | GL | 10 | H |  |  | 380 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | P2 | 56 |  | 380 |  | GL | 10 | O |  |  | 380 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | P3 | 56 |  | 400 |  | T | 10 | O |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | P3 | 56 |  | 410 |  | T | 10 | H |  |  | 410 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | P3 | 56 |  | 390 |  | GL | 10 | H |  |  | 390 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | P3 | 56 |  | 380 |  | GL | 10 | O |  |  | 380 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | P4 | 56 |  | 410 |  | T | 10 | H |  |  | 410 |  |  |  | 0 |  | 1 |  |  |  | CS2 10mm crack under H2 seat, band fitted |  |  |  |  |  |  |
| O | P1 | P4 | 56 |  | 350 |  | T | 10 | O |  |  | 350 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | P4 | 56 |  | 350 |  | GL | 10 | O |  |  | 350 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P1 | P4 | 56 |  | 310 |  | GL | 10 | H |  |  | 310 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G1 | 22 |  | 360 |  | E1 | 10 | H |  |  | 360 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G1 | 22 |  | 360 |  | S1 | 10 |  |  |  |  |  |  |  |  |  | 4 |  |  | 60 | CS2 Band fitted |  |  |  |  |  |  |
| O | S2 | G1 | 22 |  | 360 |  | MS | 10 | H |  |  | 360 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G1 | 22 |  | 350 |  | MS | 10 | V |  |  | 350 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G1 | 22 |  | 360 |  | E2 | 10 | H |  |  | 360 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G1 | 22 |  | 365 |  | S2 | 10 |  |  |  |  |  |  |  |  |  | 4 |  |  | 60 | CS2 Bands fitted |  |  |  |  |  |  |
| O | S2 | G2 | 22 |  | 360 |  | E1 | 10 | H |  |  | 360 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G2 | 22 |  | 370 |  | S1 | 10 |  |  |  |  |  |  |  |  |  | 1 |  |  | 20 |  |  |  |  |  |  |  |
| O | S2 | G2 | 22 |  | 375 |  | MS | 10 | H |  |  | 375 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G2 | 22 |  | 395 |  | MS | 10 | V |  |  | 395 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G2 | 22 |  | 380 |  | E2 | 10 | H |  |  | 380 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G2 | 22 |  | 370 |  | S2 |  |  |  |  |  |  |  |  |  |  | 2 |  |  | 25 |  |  |  |  |  |  |  |
| O | S2 | G3 | 22 |  | 395 |  | E1 | 10 | H |  |  | 395 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G3 | 22 |  | 395 |  | S1 |  |  |  |  |  |  |  |  |  |  | 1 |  |  | 20 |  |  |  |  |  |  |  |
| O | S2 | G3 | 22 |  | 400 |  | MS | 10 | H |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G3 | 22 |  | 400 |  | MS | 10 | V |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G3 | 22 |  | 400 |  | E2 | 10 | H |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G3 | 22 |  | 400 |  | S2 |  |  |  |  |  |  |  |  |  |  | 2 |  |  | 25 |  |  |  |  |  |  |  |
| O | S2 | G4 | 22 |  | 420 |  | E1 | 10 | H |  |  | 420 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G4 | 22 |  | 400 |  | S1 |  |  |  |  |  |  |  |  |  |  | 3 |  |  | 50 | CS2 Bands fitted |  |  |  |  |  |  |
| O | S2 | G4 | 22 |  | 430 |  | MS | 10 | H |  |  | 430 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G4 | 22 |  | 470 |  | MS | 10 | V |  |  | 470 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G4 | 22 |  | 400 |  | E2 | 10 | H |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G4 | 22 |  | 415 |  | S2 |  |  |  |  |  |  |  |  |  |  | 1 |  |  | 20 |  |  |  |  |  |  |  |
| O | S2 | G5 | 22 |  | 355 |  | E1 | 10 | H |  |  | 355 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G5 | 22 |  | 320 |  | S1 |  |  |  |  |  |  |  |  |  |  | 3 |  |  | 35 | CS2 Bands fitted |  |  |  |  |  |  |
| O | S2 | G5 | 22 |  | 350 |  | MS | 10 | H |  |  | 350 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G5 | 22 |  | 330 |  | MS | 10 | V |  |  | 330 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G5 | 22 |  | 340 |  | E2 | 10 | H |  |  | 340 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S2 | G5 | 22 |  | 320 |  | S2 |  |  |  |  |  |  |  |  |  |  | 3 |  |  | 35 |  |  |  |  |  |  |  |
| O | P2 | COR1 | 27 |  | 360 |  | E1 | 10 | H |  |  | 360 |  |  |  | 0 |  | 1 |  |  |  | Gang nails fitted on both ends |  |  |  |  |  |  |
| O | P2 | COR1 | 27 |  | 255 |  | E1 | 10 | V |  |  | 255 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | COR1 | 27 |  | 360 |  | O | 10 | H |  |  | 360 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound mid-cor. |  |  |  |  |  |  |
| O | P2 | COR1 | 27 |  | 335 |  | E2 | 10 | H |  |  | 335 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | COR1 | 27 |  | 255 |  | E2 | 10 | V |  |  | 255 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | COR2 | 27 |  | 400 |  | E1 | 10 | H |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  | Gang nails fitted both ends |  |  |  |  |  |  |
| O | P2 | COR2 | 27 |  | 305 |  | E1 | 10 | V |  |  | 305 |  |  |  | 0 |  | 1 |  |  |  | 20mm packers between COR & h/stocks. |  |  |  |  |  |  |
| O | P2 | COR2 | 27 |  | 400 |  | O | 10 | H |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound mid-cor. |  |  |  |  |  |  |
| O | P2 | COR2 | 27 |  | 400 |  | E2 | 10 | H |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | COR2 | 27 |  | 310 |  | E2 | 10 | V |  |  | 310 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | COR3 | 27 |  | 390 |  | E1 | 10 | H |  |  | 390 |  |  |  | 0 |  | 1 |  |  |  | Gang nails fitted both ends |  |  |  |  |  |  |
| O | P2 | COR3 | 27 |  | 310 |  | E1 | 10 | V |  |  | 310 |  |  |  | 0 |  | 1 |  |  |  | 10mm packer between COR & h/stocks |  |  |  |  |  |  |
| O | P2 | COR3 | 27 |  | 390 |  | O | 10 | H |  |  | 390 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound mid-cor. |  |  |  |  |  |  |
| O | P2 | COR3 | 27 |  | 375 |  | E2 | 10 | H |  |  | 375 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | COR3 | 27 |  | 310 |  | E2 | 10 | V |  |  | 310 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | COR4 | 27 |  | 415 |  | E1 | 10 | H |  |  | 415 |  |  |  | 0 |  | 1 |  |  |  | Gang nails fitted both ends |  |  |  |  |  |  |
| O | P2 | COR4 | 27 |  | 290 |  | E1 | 10 | V |  |  | 290 |  |  |  | 0 |  | 1 |  |  |  | 10mm packers between COR & h/stock |  |  |  |  |  |  |
| O | P2 | COR4 | 27 |  | 415 |  | O | 10 | H |  |  | 415 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound mid-cor. |  |  |  |  |  |  |
| O | P2 | COR4 | 27 |  | 385 |  | E2 | 10 | H |  |  | 385 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | COR4 | 27 |  | 325 |  | E2 | 10 | V |  |  | 325 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | COR5 | 27 |  | 365 |  | E1 | 10 | H |  |  | 365 |  |  |  | 0 |  | 1 |  |  |  | Gang nails fitted both ends |  |  |  |  |  |  |
| O | P2 | COR5 | 27 |  | 260 |  | E1 | 10 | V |  |  | 260 |  |  |  | 0 |  | 1 |  |  |  | 10mm packers between COR & h/stocks |  |  |  |  |  |  |
| O | P2 | COR5 | 27 |  | 365 |  | O | 10 | H |  |  | 365 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound mid-cor. |  |  |  |  |  |  |
| O | P2 | COR5 | 27 |  | 350 |  | E2 | 10 | H |  |  | 350 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | COR5 | 27 |  | 255 |  | E2 | 10 | V |  |  | 255 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | H1 | 54 |  | 175 |  | E1 | 10 | H |  |  | 175 |  |  |  | 0 |  | 2 |  |  |  | Bands & end caps fitted both ends |  |  |  |  |  |  |
| O | P2 | H1 | 54 |  | 175 |  | O1 | 10 | H |  |  | 175 |  |  |  | 0 |  | 2 |  |  |  | Drilled sound at P2 & P3 |  |  |  |  |  |  |
| O | P2 | H1 | 54 |  | 175 |  | E2 | 10 | H |  |  | 175 |  |  |  | 0 |  | 2 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | H2 | 54 |  | 210 |  | E1 | 10 | H |  |  | 210 |  |  |  | 0 |  | 1 |  |  |  | Treated, bands & end caps fitted both ends |  |  |  |  |  |  |
| O | P2 | G2 | 54 |  | 210 |  | O | 10 | H |  |  | 210 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound at P2 & P3 |  |  |  |  |  |  |
| O | P2 | H2 | 54 |  | 210 |  | E1 | 10 | V |  |  | 210 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | P1 | 56 |  | 420 |  | T | 10 | H |  |  | 420 |  |  |  | 0 |  | 1 |  |  |  | CS2 Whiterot & sap loss |  |  |  |  |  |  |
| O | P2 | P1 | 56 |  | 440 |  | T | 10 | O |  |  | 440 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | P1 | 56 |  | 340 |  | GL | 10 | H |  |  | 340 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | P1 | 56 |  | 360 |  | GL | 10 | O |  |  | 360 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | P2 | 56 |  | 390 |  | T | 10 | H |  |  | 390 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | P2 | 56 |  | 410 |  | T | 10 | O |  |  | 410 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | P2 | 56 |  | 350 |  | GL | 10 | H |  |  | 350 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | P2 | 56 |  | 350 |  | GL | 10 | O |  |  | 350 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | P3 | 56 |  | 380 |  | T | 10 | H |  |  | 310 |  | 70 |  | 18 |  | 2 |  |  |  | CS2 Sap loss. Pipe possibly crack |  |  |  |  |  |  |
| O | P2 | P3 | 56 |  | 370 |  | T | 10 | O |  |  | 325 |  | 45 |  | 12 |  | 2 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | P3 | 56 |  | 320 |  | GL | 10 | H |  |  | 320 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | P3 | 56 |  | 330 |  | GL | 10 | O |  |  | 330 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | P4 | 56 |  | 450 |  | T | 10 | H |  |  | 450 |  |  |  | 0 |  | 1 |  |  |  | CS2 Sap loss |  |  |  |  |  |  |
| O | P2 | P4 | 56 |  | 455 |  | T | 10 | O |  |  | 455 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | P4 | 56 |  | 420 |  | GL | 10 | H |  |  | 420 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | P2 | P4 | 56 |  | 410 |  | GL | 10 | O |  |  | 410 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G1 | 22 |  | 390 |  | E1 | 10 | H |  |  | 390 |  |  |  | 0 |  | 1 |  |  |  | CS2 Sawn, treated |  |  |  |  |  |  |
| O | S3 | G1 | 22 |  | 400 |  | E1 | 10 | V |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G1 | 22 |  | 400 |  | MS | 10 | H |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G1 | 22 |  | 410 |  | MS | 10 | V |  |  | 410 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G1 | 22 |  | 410 |  | E2 | 10 | H |  |  | 410 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound on very end, 100mm from ABS |  |  |  |  |  |  |
| O | S3 | G1 | 22 |  | 400 |  | S2 |  |  |  |  |  |  |  |  |  |  | 2 |  |  | 30 |  |  |  |  |  |  |  |
| O | S3 | G2 | 22 |  | 390 |  | E1 | 10 | H |  |  | 390 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G2 | 22 |  | 390 |  | S1 |  |  |  |  |  |  |  |  |  |  | 2 |  |  | 30 |  |  |  |  |  |  |  |
| O | S3 | G2 | 22 |  | 395 |  | MS | 10 | H |  |  | 395 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G2 | 22 |  | 400 |  | MS | 10 | V |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G2 | 22 |  | 400 |  | E2 | 10 | H |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound on very end, 100mm from ABS |  |  |  |  |  |  |
| O | S3 | G2 | 22 |  | 400 |  | S2 |  |  |  |  |  |  |  |  |  |  | 2 |  |  | 25 | 10mm packers between girder & h/stock |  |  |  |  |  |  |
| O | S3 | G2 | 22 |  | 395 |  | E1 | 10 | H |  |  | 395 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G3 | 22 |  | 400 |  | S1 |  |  |  |  |  |  |  |  |  |  | 2 |  |  | 35 |  |  |  |  |  |  |  |
| O | S3 | G3 | 22 |  | 395 |  | MS | 10 | H |  |  | 395 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G3 | 22 |  | 405 |  | MS | 10 | V |  |  | 405 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G3 | 22 |  | 385 |  | E2 | 10 | H |  |  | 385 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound on very end, 100mm from ABS |  |  |  |  |  |  |
| O | S3 | G3 | 22 |  | 385 |  | S2 |  |  |  |  |  |  |  |  |  |  | 2 |  |  | 30 | 30mm packer between girder & h/stock |  |  |  |  |  |  |
| O | S3 | G4 | 22 |  | 385 |  | E1 | 10 | H |  |  | 385 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G4 | 22 |  | 385 |  | S1 |  |  |  |  |  |  |  |  |  |  | 2 |  |  | 40 |  |  |  |  |  |  |  |
| O | S3 | G4 | 22 |  | 395 |  | MS | 10 | H |  |  | 395 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G4 | 22 |  | 385 |  | MS | 10 | V |  |  | 385 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G4 | 22 |  | 395 |  | E2 | 10 | H |  |  | 335 |  | 60 |  | 15 |  | 2 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G4 | 22 |  | 390 |  | E2 | 10 | V |  |  | 330 |  | 60 |  | 15 |  | 2 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G4 | 22 |  | 390 |  | S2 |  |  |  |  |  |  |  |  |  |  | 2 |  |  | 30 | CS2 20mm packer between girder & h/stock |  |  |  |  |  |  |
| O | S3 | G4 | 22 |  | 390 |  | O | 10 | H |  |  | 305 |  | 85 |  | 22 |  | 2 |  |  |  | Drilled on very end, 100mm from ABS |  |  |  |  |  |  |
| O | S3 | G5 | 22 |  | 415 |  | E1 | 10 | H |  |  | 415 |  |  |  | 0 |  | 1 |  |  |  | Sawn, treated |  |  |  |  |  |  |
| O | S3 | G5 | 22 |  | 405 |  | E1 | 10 | V |  |  | 405 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G5 | 22 |  | 415 |  | MS | 10 | H |  |  | 415 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G5 | 22 |  | 410 |  | MS | 10 | V |  |  | 410 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | S3 | G5 | 22 |  | 415 |  | E2 | 10 | H |  |  | 415 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound on very end, 100mm from ABS |  |  |  |  |  |  |
| O | S3 | G5 | 22 |  | 400 |  | E2 | 10 | V |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A2 | H1 | 54 |  | 175 |  | E1 | 10 | H |  |  | 175 |  |  |  | 0 |  | 2 |  |  |  | Minor cracking, bands fitted both ends |  |  |  |  |  |  |
| O | A2 | H1 | 54 |  | 175 |  | O | 10 | H |  |  | 175 |  |  |  | 0 |  | 2 |  |  |  | Drilled sound at P2 & P3 |  |  |  |  |  |  |
| O | A2 | H1 | 54 |  | 175 |  | E2 | 10 | H |  |  | 175 |  |  |  | 0 |  | 2 |  |  |  | Weathering |  |  |  |  |  |  |
| O | A2 | H2 | 54 |  | 300 |  | E1 | 10 | V |  |  | 300 |  |  |  | 0 |  | 1 |  |  |  | Treated, bands & end caps fitted both ends |  |  |  |  |  |  |
| O | A2 | H2 | 54 |  | 300 |  | O1 | 10 | V |  |  | 300 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound at P2 & P3 |  |  |  |  |  |  |
| O | A2 | H2 | 54 |  | 300 |  | E2 | 10 | V |  |  | 300 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A2 | P1 | 60 |  | 340 |  | T | 10 | H |  |  | 140 |  | 200 |  | 59 |  | 4 |  |  |  | Cracking (600mm visible) |  |  |  |  |  |  |
| O | A2 | P1 | 60 |  | 360 |  | T | 10 | O |  |  | 240 |  | 120 |  | 33 |  | 3 |  |  |  |  |  |  |  |  |  |  |
| O | A2 | P2 | 60 |  | 350 |  | T | 10 | H |  |  | 300 |  | 50 |  | 14 |  | 2 |  |  |  | CS4 Fire damage at top (800mm visible) |  |  |  |  |  |  |
| O | A2 | P2 | 60 |  | 350 |  | T | 10 | O |  |  | 230 |  | 120 |  | 34 |  | 3 |  |  |  |  |  |  |  |  |  |  |
| O | A2 | P2 | 60 |  | 300 |  | GL | 10 | H |  |  | 300 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A2 | P1 | 56 |  | 390 |  | T | 10 | H |  |  | 390 |  |  |  | 0 |  | 1 |  |  |  | CS2 Butt spliced at GL (4 x plates fitted) |  |  |  |  |  |  |
| O | A2 | P1 | 56 |  | 350 |  | T | 10 | O |  |  | 350 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A2 | P1 | 56 |  | 380 |  | GL | 10 | H |  |  | 380 |  |  |  | 0 |  | 1 |  |  |  | Drilled sound above & below splice |  |  |  |  |  |  |
| O | A2 | P1 | 56 |  | 350 |  | GL | 10 | O |  |  | 350 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A2 | P2 | 56 |  | 425 |  | T | 10 | H |  |  | 425 |  |  |  | 0 |  | 1 |  |  |  | CS2 Sap loss (700mm visible) |  |  |  |  |  |  |
| O | A2 | P2 | 56 |  | 405 |  | T | 10 | O |  |  | 405 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A2 | P3 | 56 |  | 410 |  | T | 10 | H |  |  | 410 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A2 | P3 | 56 |  | 400 |  | T | 10 | O |  |  | 400 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A2 | P4 | 56 |  | 430 |  | T | 10 | H |  |  | 370 |  | 60 |  | 14 |  | 2 |  |  |  | CS2 12mm crack has band fitted (200mm visible) |  |  |  |  |  |  |
| O | A2 | P4 | 56 |  | 400 |  | T | 10 | O |  |  | 360 |  | 40 |  | 10 |  | 2 |  |  |  |  |  |  |  |  |  |  |
| O | A2 | P3 | 60 |  | 280 |  | T | 10 | H |  |  | 280 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |
| O | A2 | P3 | 60 |  | 310 |  | T | 10 | O |  |  | 310 |  |  |  | 0 |  | 1 |  |  |  |  |  |  |  |  |  |  |